COATED BACKLIT PROFLEX BANNER

| Property | Unit | Test Method |
| --- | --- | --- |
| Yarn Type. | 1000D/ Polyester |  |
| Base fabric | 1000x1000 20x20 | DIN EN ISO 2060 |
| Weight | 510 gsm +/- 5% | DIN EN ISO 2286-2 |
| Tensile Strength | 2200 x 1850 N/5cm | DIN EN ISO 1421 |
| Tear Strength | 30/250 N | DIN 53363 |
| Coating | Coated Backlit, Smooth surfaces both sides |  |
| Ink Suitability | Solvent, Eco-solvent, UV, Screen printing |  |
| Width | 3200mm |  |
| Roll Length | 50 metres (nominal) |