COATED MESH PROFLEX BANNER

| Property | Unit | Test Method |
| --- | --- | --- |
| Yarn Type. | 1000D/ Polyester |  |
| Base fabric | 9x3 weave | DIN EN ISO 2060 |
| Weight | 270 gsm +/- 5% | DIN EN ISO 2286-2 |
| Tensile Strength | 1250 x 1350 N/5cm | DIN EN ISO 1421 |
| Tear Strength | 330/320 N | DIN 53363 |
| Coating | Coated Mesh |  |
| Ink Suitability | Solvent, Eco-solvent, UV, Screen printing |  |
| Width | 3200mm |  |
| Roll Length | 50 metres (nominal) |

Film backed to stop ink running through