| Property | Unit | Test Method |
| --- | --- | --- |
| Yarn Type. | 1100D/Tex Polyester | DIN 53830 |
| Base fabric | 20x20 weave |  |
| Weight | 610 gsm +/- 5% | DIN 53352 |
| Tensile Strength | 1640 x 1480 N/25cm | DIN 53354 |
| Tear Strength | 270x250 | DIN 53363 |
| Coating | PVC Spread Coating |  |
| Surface | Acrylic Lacquer Coating |
| Adhesion | 60N/25cm | DIN 53357 |
| Fire Retardant | Yes | AS 1530 Pt 2 |
| Width | 250cm |  |
| Roll Length | 40 metres (nominal) |

Warranty                                            3 Year UV warranty